P r o d u c t  D a t a  s h e e t

G 2 8 5 5

H i g h D e n s i t y P o l y e t h y l e n e ( H D P E )

Description:

G2855 is a High Density Polyethylene resin for blow molding with good impact strength, medium  stiffness.   It  is  suitable  for  container  a  few ml  to  20 liters,  lubricant  or  cosmetic bottle,  chemical  container,  one-way bottle.  It  also  meets  the  F.D.A.  requirement  in  the code of federal regulations in 21 CFR 177.1520 for food contact.

Physical Properties: Method Unit Value

Melt Flow Index (2.16 kg/190⁰C) ASTM D1238 g/10min. 0.35

Melt Flow Index (5 kg/190DC) ASTM D1238 g/10min. 1.50

Density ASTM D792 g/cm3 0.955

Tensile Strength at Yield ASTM D638 MPA 29.5

Tensile Strength at Break ASTM D638 MPA 33

Ultimate Elongation ASTM D638 % 2000

Hardness Shore D DIN 53505 - 65

Charpy Notched Impact Strength (at 23⁰C) DIN 53453 mJ/mm2 7.5

Vicat Softening Temperature ASTM D1525 ⁰C 125

Environmental Stress Cracking Resistance (condition B, F50) ASTM D1693 hours 60

Processing Technique

Processing Temperature : 170 – 200 °C

**However, the actual processing conditions depend on machine and other environments.**

Remark: The values presented on the above are typical laboratory average, not to be construed as specifications and may vary within moderate ranges. The applicability or the accuracy of this information or the suitable of our products cannot be guaranteed because the conditions of use on the part or our uses are beyond our control.

REV. 20110601